PMID: 19576609 [PubMed - indexed for MEDLINE]

Water Res. 2009 Aug;43(15):3659-72. Epub 2009 Jun 6.

# Simultaneous removal of Cu, Mn and Zn from drinking water with the use of clinoptilolite and its Fe-modified form.

Doula MK.

National Agricultural Research Foundation of Greece, Soil Science Institute of Athens, 1 Sof. Venizelou St., Lycovrisi, Greece. mdoula@otenet.gr

Zeolites have been widely used in water treatment and especially clinoptilolite, due to its low cost and high abundance. It has large cation-exchange capacity and is capable of removing large quantities of heavy metals from contaminated water samples. By loading the surface of clinoptilolite with amorphous Fe-oxide species, a total improvement in adsorption capacity could be achieved. Thus, the Clin-Fe oxide system is capable of adsorbing significantly higher heavy metal concentrations than untreated clinoptilolite with simultaneous noticeable decrease in water hardness. Batch adsorption experiments have shown that Clin-Fe system has very large Cu, Zn and Mn adsorption capacity and for most of the cases the treated water samples were suitable for human consumption or agricultural use. New experiments were conducted to study the effectiveness of clinoptilolite and of the Clin-Fe system in removal of Cu, Mn, Zn, present simultaneously in water samples, so that the study of metal-sorbent chemical behavior and of the adsorption selectivity would be feasible. Desorption of metals was also examined and an integrated approach of the effectiveness of such materials in drinking water treatment is presented.