Zeolite a inhibits osteoclast-mediated bone resorption in vitro

N. Schütze 1, M. J. Oursler 1, J. Nolan 3, B. L. Riggs 2, T. C. Spelsberg Dr. 1 *

1Departments of Biochemistry and Molecular Biology, Mayo Clinic and Mayo Foundation, Rochester, Minnesota 55905
2Endocrine Research Unit, Mayo Clinic and Mayo Foundation, Rochester, Minnesota 55905
3Whiteby Inc., Richmond, Virginia 23261-5054

Correspondence to T. C. Spelsberg Dr., Department of Biochemistry and Molecular Biology, Mayo Clinic, 200 First Street SW, Rochester, MN 55905

Keywords

Zeolite A • resorption • Qsteoclasts • Cathepsins • Silicon deoxide • aluminum chloride • osteoporosis

Abstract

The effects of Zeolite A on Bone resorbing activity of highly purified avian osteoclasts were analyzed. The present study demonstrates that when 100 pg/ml of acid-treated Zeolite A is added to the media the number of pits per osteoclast is reduced 3-fold at 24h after treatment. Secreted cathepsin B enzyme activity was also reduced 3-fold. A similar reduction in pit number per osteoclast was measured following 48 h of treatment with Zeolite A but there appeared to be less reduction of cathepsin B enzyme activity. The effects on pit number and cathepsin B Protein activity were Zeolit dose dependent. The structure of the compound seemed to be responsible for the effects measured since compounds used to represent constituents of Zeolite A (silicon dioxide and aluminum cholride) failed to inhibit bone resorption or reduce the level of secreted cathepsin B enzyme activity. Thus the molicular architecture of Zeolite A or a derivative there of appears to be inportant. In conclusion, the data indicate that Zeolite A can inhibit bone resorption. Together with previous data on osteoblasts, this might suggest a potential positive activity of intact Zeolite A or a partial substructure of Zeolite A on bone turnover. © Wiley-Liss, Inc.